Summer Internship Programme – PGDM – ISME25-27

Assignment Report  |  Steel & Construction Division

| Intern: K. Mohammed Abdulla Khan Roll no: 2511421 | Organisation: Hindupur steels and alloys (P) Ltd. | Period: SIP Week 1&2 |
| --- | --- | --- |

# 1.  Introduction to Internship / Summer Training

This internship was undertaken at Hindupur steels and alloys (P) Ltd. , a TMT bar manufacturing plant, as part of an industrial training programme in the Steel & Construction sector. The training spanned from April 2 to April 13, 2026, covering two progressive weeks of hands-on exposure to the complete TMT bar production process — from raw material procurement and elemental testing, through smelting and billet casting, to rolling, quenching, and final quality control testing.

The Grade Testing Laboratory is an integral in-house quality control unit within the Hindupur steels and alloys (P) Ltd.  plant. It conducts mandatory tensile testing of produced rebar every 30 minutes during active production runs of 8 mm, 12 mm, and 20 mm diameter TMT bars, ensuring each batch meets IS 1786 mechanical property requirements before dispatch. The internship thus provided end-to-end exposure — from the raw material stage at the Spectro Lab and smelter, all the way through to finished product verification at the Grade Testing Lab.

# 2.  Relevance of Topic

TMT (Thermo-Mechanically Treated) bars are the single most critical material in reinforced concrete construction — used in buildings, bridges, dams, and roads across India. The relevance of this internship spans several key dimensions:

- Structural Safety: Understanding tensile strength, yield stress, and elongation % is essential for ensuring that rebars meet the mechanical property requirements of IS 1786 : 2008. The observed sample (20 mm bar) recorded a Yield Stress of 542 N/mm² and a Tensile Strength of 644 N/mm², confirming Fe 500 grade compliance.

- Quality at Source: The entire production chain at Hindupur steels and alloys (P) Ltd.  relies on real-time Spectro Lab analysis (results in 5–10 seconds) to verify elemental composition of raw materials before any large-scale melting is commenced.

- Seismic Resilience: The Ring Test (Etching Test) reveals the three-zone microstructure — Tempered Martensite outer ring, Bainite transition zone, and Ferrite-Pearlite core — whose balance determines both the strength and ductility of the bar. This is directly relevant to earthquake-resistant construction governed by IS 1893 and IS 13920.

- Industry Economics: Power cost calculations observed during smelter operations (₹3.89 lakh per 18-tonne billet batch at ₹6/unit) illustrate the real cost pressures that drive quality-efficiency decisions on the production floor.

- Standards Compliance: IS 1786 tolerance ranges (±7% for 8–10 mm, ±5% for 12–16 mm, ±3% for 20 mm and above) directly impact procurement, quality rejection, and structural design calculations.

# 3.  Theoretical Background

## 3.1  TMT Bar Manufacturing & Microstructure

TMT bars are produced by passing hot-rolled steel through a quenching water-jet system immediately after the rolling mill. The outer surface cools rapidly, forming a hard martensite shell, while the core remains hot and ductile. Upon air cooling, the residual heat from the core tempers the outer martensite (self-tempering), resulting in three distinct microstructural zones:

| Zone | Crystal Structure | Appearance | Function |
| --- | --- | --- | --- |
| Tempered Martensite (outer ring) | Fine lath martensite | Dark / Black | High tensile strength |
| Transition Zone (middle band) | Bainite / Mixed | Medium / Brown | Toughness & shock absorption |
| Ferrite-Pearlite Core (inner) | Ferrite + Pearlite (soft) | Light / White | Ductility & flexibility |

## 3.2  Ring Test (IS 1786 : 2008) — Etching Test

The Ring Test verifies the microstructure of a TMT bar by cutting a cross-section, polishing it smooth, and applying 5–10% Nital solution (nitric acid in ethanol) for 15–30 seconds. The chemical etches each zone differently: the martensite ring appears dark/black, the transition zone medium-brown, and the ferrite-pearlite core appears light. A continuous, unbroken dark outer ring constitutes a PASS; any break or unevenness in the ring indicates an uneven quench (FAIL), and the bar must be rejected.

## 3.3  Tensile Testing & Mechanical Properties

Tensile testing is conducted every 30 minutes during production. Key parameters measured include Yield Load, Tensile Load, Cross-Sectional Area (CSA), Yield Stress, Tensile Strength, T.S./Y.S. ratio, and Elongation %. The sample recorded during training (20 mm bar equivalent): Yield Stress 542 N/mm², Tensile Strength 644 N/mm², T.S./Y.S. ratio 1.20, and Elongation 18–10% — all consistent with Fe 500D grade requirements under IS 1786. The weight formula D²/162 (kg/m) is used to cross-check dimensional compliance, with IS 1786 tolerances of ±7% (8–10 mm), ±5% (12–16 mm), and ±3% (20 mm and above).

## 3.4  Raw Material Testing & Smelter Operations

Before any raw material (scrap iron, sponge iron, pig iron, gypsum) enters the furnace, a lollipop-shaped sample is prepared, polished flat, and tested in the Spectro Lab (precision ±10–15 units, results in 5–10 seconds). If results fail, the material is rejected or sent to the Chemical Lab for 3-hour confirmatory analysis. The smelter processes a minimum of 15–20 tonnes per cycle, producing 18-tonne billet batches (∼90% yield) at a melt temperature of ∼1380°C, consuming approximately 722 kWh per tonne. The molten steel is then cast into billets by the CCM (Continuous Casting Machine) unit, completing the raw-material-to-billet transformation before TMT rolling begins.

## 3.5  TMT Bar Size, Area, Volume & Bundle Reference Chart

The following chart is derived from the plant's reference spreadsheet (Size_and_bundle_chart.xlsx). Calculations use π = 3.14, Density of iron = 0.00785 g/mm³, and standard bar length = 11 m. The weight per metre is computed using the industry formula: Weight (kg/m) = D² ÷ 162, where D is the diameter in mm. Area and Volume are derived from first principles (Area = π × r²; Volume per unit length = Area × Density).

| Area (mm²) = π × r² = 3.14 × (D/2)² | Volume (g/mm length) = Area × Density (0.00785) | Weight per metre (kg/m) = D² ÷ 162 (simplified formula) |
| --- | --- | --- |

| Size | Dia (mm) | Radius (mm) | Area (mm²) | Volume (g/mm) | Wt/m (kg) | Wt/11m (kg) | Qty / Bundle | Bundle Wt (kg) | IS 1786 Tol. | + Max (kg) | − Min (kg) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 8mm | 8 | 4 | 50.24 | 0.3944 | 0.395 | 4.345 | 10 | 43.45 | ±7% | 46.49 | 40.41 |
| 10mm | 10 | 5 | 78.5 | 0.6162 | 0.617 | 6.787 | 7 | 47.51 | ±7% | 50.84 | 44.18 |
| 12mm | 12 | 6 | 113.04 | 0.8874 | 0.889 | 9.779 | 5 | 48.9 | ±5% | 51.34 | 46.45 |
| 16mm | 16 | 8 | 200.96 | 1.5775 | 1.58 | 17.38 | 3 | 52.14 | ±5% | 54.75 | 49.53 |
| 20mm | 20 | 10 | 314 | 2.4649 | 2.469 | 27.159 | 2 | 54.32 | ±3% | 55.95 | 52.69 |
| 25mm | 25 | 12.5 | 490.62 | 3.8514 | 3.858 | 42.438 | 1 | 42.44 | ±3% | 43.71 | 41.17 |
| 32mm | 32 | 16 | 803.84 | 6.3101 | 6.321 | 69.531 | 1 | 69.53 | ±3% | 71.62 | 67.45 |
| 44mm | 44 | 22 | 1519.76 | 11.93 | 11.951 | 131.461 | 1 | 131.46 | N/A | - | - |

This assignment report is a true summary of observations and learnings from the internship at Hindupur steels and alloys (P) Ltd. , SIPWeek 1&2

Submitted By: K. Mohammed Abdulla Khan – 2511421